## Slide 1
 | S1 | S2 | S3 | … | Si
ω1 | i.j matrix of data points |  |  |  | 
ω2 |  |  |  |  | 
ω3 |  |  |  |  | 
… |  |  |  |  | 
ωj |  |  |  |  | 
 | S1 | S2 | S3 | … | Si
PC1 | i.k (k≤j) matrix of data points |  |  |  | 
PC2 |  |  |  |  | 
PC3 |  |  |  |  | 
… |  |  |  |  | 
PCk |  |  |  |  | 
J1
J2
J3
J…
Ji
J1
J2
J3
J…
Ji
PC1
PC2
PC3
PC1
PC3
PC…
PCk
PC2
HOW PCA WORKS

## Slide 2
XYZ Stage
Obj
Raman setup
Laser
CCD
Mirror
Lens
Dichroic
Filter
(long pass)
Diffraction
grating
Microscope
785 RazorEdge Filter
# LPO2-785RU-25
785 RazorEdge Dichroic Beamsplitter
# LPDO2-785RU-25

## Slide 3
Within
Between
Between
Within
HOW LDA WORKS

## Slide 4
JABLONSKI DIAGRAM
Energy
Infrared
UV/Visible
Spontaneous
Stimulated
Absorption
Emission
Scattering
Rayleigh
Stokes
Anti-Stokes
Inelastic
Elastic
S0
S1
Virtual
State
ν0
ν1
ν2
ν0
ν1
ν2

## Slide 5
CO2 VIBRATIONAL MODES

## Slide 6
Oscillating displacement of plasma
-
-
-
-
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
+
+
+
+
+
Electric field
Time
AuNP

## Slide 7
Parallel vs perpendicular dimer
E
E

## Slide 8
NP Hybridisation
Θi
θj
*
l = 2
l = 1
l = 1
l = 2
d
xi

## Slide 9
Energy transfer in EM SERS
E
Ef
HOMO
LUMO
Analyte

## Slide 10
LBL Prep & diagram
Polystyrene
AuNP
PEI
PSS
3x Polyelectrolyte layer
1 hour
soak in
AuNPs
Collect sensors
10 minute
soak in PEI
10 minute
soak in PSS

## Slide 11
Chart: Wavelength (nm)
TEM & LM Images
A
B
C
D

## Slide 12
Scattering timecourse
RSD (%)
633nm = 6.45
785nm = 5.83
RSD (%)
633nm = 11.70
785nm = 14.51

## Slide 13
Chart: Time (min)
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
AuNPs 633nm | 0.20777 | 0.16797 | 0.1594 | 0.15684 | 0.15392 | 0.14964 | 0.14176 | 0.14396 | 0.14087 | 0.15795 | 0.16129
AuNPs 785nm | 0.30031 | 0.23702 | 0.22236 | 0.21656 | 0.21321 | 0.20069 | 0.18925 | 0.19137 | 0.18765 | 0.21528 | 0.21632
LBL 633nm | 0.32111 | 0.29972 | 0.28204 | 0.3054 | 0.27533 | 0.27398 | 0.28643 | 0.3002 | 0.33159 | 0.32074 | 0.29442
LBL 785nm | 0.36324 | 0.33986 | 0.3239 | 0.34926 | 0.31779 | 0.31954 | 0.32913 | 0.3494 | 0.37629 | 0.36714 | 0.33547
Scattering cont.

## Slide 14
Peak (cm-1) | Standard deviation in intensity |  | Relative standard deviation (%) | 
 | 40nm AuNP | LBL | 40nm AuNP | LBL
1075 | 32.1 | 44.6 | 10.9 | 3.1
1585 | 27.6 | 71.9 | 15.0 | 5.8
A
C
D
B
LBL
AuNP
Chart: Time (Min)
| 0 | 0.5 | 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6 | 6.5 | 7 | 7.5 | 8 | 8.5 | 9
LBL 1075nm | 1519.66 | 1503.54 | 1472.67 | 1450.97 | 1480.58 | 1491.97 | 1502.69 | 1461.92 | 1474.6 | 1445.38 | 1469.19 | 1471.06 | 1413.08 | 1422.56 | 1400.98 | 1416.99 | 1399.22 | 1376.8 | 1376.42
LBL 1585nm | 1345.21 | 1324.73 | 1290.83 | 1302.77 | 1312.2 | 1305.41 | 1294.42 | 1294.24 | 1243.57 | 1237.79 | 1244.32 | 1203.91 | 1190.86 | 1199.24 | 1151.68 | 1138.83 | 1147.77 | 1163.1 | 1139.79
AuNP 1075nm | 266.343 | 274.698 | 318.73 | 278.454 | 305.71 | 262.332 | 271.216 | 298.684 | 284.783 | 272.264 | 288.774 | 294.255 | 291.146 | 299.923 | 397.959 | 343.478 | 264.714 | 303.247 | 287.818
AuNP 1585nm | 146.813 | 156.661 | 186.872 | 165.798 | 181.439 | 159.808 | 159.916 | 181.575 | 175.621 | 168.648 | 176.379 | 189.107 | 182.756 | 219.514 | 263.054 | 224.42 | 169.734 | 202.619 | 183.218

## Slide 15
D
A
B
C